## Slide 1: MSFfit Overview
Notes: In this presentation:
The relationship between the plasticity-damage model (DMG), and the model calibration tool (DMGfit)
Implementations of DMGfit: for users on stand-alone PCs, or for Web-based users
The overall model calibration strategy
The calibration process specific to the DMG
The mapping of the calibration process to the DMGfit GUI
Labor saving features in the GUI, requested by MSU researchers
DMGfit demo

## Slide 2
MSFfit – Calibration tool for the MSU Multi-Stage Fatigue model, v0.3
MSFfit Web
Service
Material Properties Repository
http://ccg.hpc.msstate.edu/cmd
Outputs:
- Model Constants
M.F. Horstemeyer
R.L. Carino
T. Haupt
Model calibration wrapper (MATLAB)
Stand-alone
MSFfit (MATLAB)
Y. Hammi
Material Point
Simulator (Fortran)
MSF UMAT
(Fortran)
Notes: DMG UMAT – model code, for ABAQUS FEA
Material Point Simulator – numerical integration routine, mimics ABAQUS for single element
Model calibration wrapper – implements the logic for model calibration
Stand-alone DMGfit – for users on Windows/Linux desktops/laptops that may not have a network connection
DMGfit web service – for users on the WWW
Material Properties Repository – a component of the CAVS-CMD CyberInfrastructure which stores experimental data, models, and model calibration tools

## Slide 3
Optimized
model constants
Good
fit ?
Yes
Generate candidate constants
No
Optimizer/Visualizer
Experimental
Strain-life data
Initial model constants
Model calibration in MSFfit
User inputs

## Slide 4: MSFfit GUI and calibration strategy
Update the GUI regions in the ff. order:
Datasets
Mechanical Properties
Microstructure
Incubation
Small crack growth
A
B
D
C
E

## Slide 5: Dataset – a text file containing name= value
fname= AA7075_data_MSF.data
excluded= 0
material= AA7075
comment= !!! EDIT THE INFO FOR THIS DATA SET !!!
strain1= 0.002
strain2= 0.02
Syld= 512
Emod= 71018
Sult= 635
DCS0= 40
DCS= 40
GO0= 3.5
GO= 3.5
poresize= 0.001
porennd= 20
partsize= 9
partdev= 4.2
porosity= 0.0015
porTH= 0.0001
(continuation)
# Experimental data
strain_amp, Nf=
0.002 4e+006
0.00225 9.70617e+006
0.0025 369280
0.0025 418700
0.0025 425100
0.0025 627594
0.00275 267145
0.003 192665
0.003 196144
0.003 289229
0.0035 105964
0.0035 132830
0.0035 136256
0.004 47500
0.004 47700
0.004 51094
0.004 52699
0.004 55600
0.004 56627
0.004 56627
(continuation)
0.005 12675
0.005 17659
0.005 17664
0.005 17931
0.005 21444
0.006 5380
0.006 5631
0.006 7169
0.007 2311
0.007 2607
0.007 2634
0.008 923
0.008 1014
0.008 1043
0.008 1084
0.01 399
0.01 429
0.01 466
0.015 84
0.015 116
0.015 150
0.02 41

## Slide 6: Typical sequence of steps
Load all experimental datasets. For each dataset, establish the experiment settings (strain Range of experiments, microstructure info) and fixed constants.
First fit the Incubation life. Some of the constants are based on physically determine constant from literature. Other constants are determined through computational studies.
Next, fit the small crack constants. Again, some of these constants are based on additional experiments and are currently determined outside of MSFfit. However, data taken from literature can be used to determine these constants.
Record results
  - Create comma separated values
  - Create a restart file

## Slide 7: Step 1
Load all experimental datasets. For each dataset, establish the experiment settings (strain range of experiments, microstructure info) and fixed constants.

## Slide 8: Load datasets
File | Load | A data file …
Select dataset

## Slide 9: Load datasets
Default on experiment 0 of 1…
Select Incubation data set to focus on…

## Slide 10: Edit plot settings
Min strain Amp .0015
Legend: NE
(northeast)
Min strain Amp .025

## Slide 11: Material constants
Strain range (data)
Mechanical Props
Microstructure Props

## Slide 12: Mechanical Properties
Yeld stress (MPa)
Elastic modulus (MPa)
Ultimate strength (MPa)

## Slide 13: Microstructure Information
Grain size/Dentrite Cell size (mm)
Texture/grain orientation
Pore size and nearest Neighbor distance (mm)
Particle size and standard deviation (mm)
Porosity and porosity threshold

## Slide 14: Step 2
First fit the Incubation stage….

## Slide 15: Incubation constants- values are default
MSFfit Default values

## Slide 16: The first dataset
Constants taken from experiments/ literature

## Slide 17: Constants from micromechanical simulations of local stress relating to incubation
Constants taken from simulations
Material Constant
Verify that these exponents are set to zero

## Slide 18: Change plot settings

## Slide 19: MSF model now shows curves for incubation, small crack and total life.

## Slide 20: Adjust CM and Alpha constants until incubation curve is optimized with the incubation data.

## Slide 21: CM= 0.2 and Alpha=-0.7 give a good correlation to the incubation experimental data.
Incubation model (dotted line) shows good agreement with experimental results

## Slide 22: Step 2
Next, fit the small crack stage….

## Slide 23: Fixed small crack growth constants
Material constant for crack tip irreversibility (0.35 for aluminum alloys)
Notes: Remember to click “Apply changes” after modifying one or more edit boxes or check boxes.

## Slide 24
DCTD threshold for pure aluminum [1]
Fixed small crack growth constants
Notes: Remember to click “Apply changes” after modifying one or more edit boxes or check boxes.

## Slide 25: Initial and final crack size: ainiC=9mm, afnl1=1000mm
Initial crack size
Final crack size
Notes: Remember to click “Apply changes” after modifying one or more edit boxes or check boxes.

## Slide 26: Multi-axial loading
Multi-axial parameter determined from experiments
Notes: Remember to click “Apply changes” after modifying one or more edit boxes or check boxes.

## Slide 27: Microstructure effects
Constants and exponents that account for grain size, porosity, texture effects

## Slide 28: Remove incubation life data

## Slide 29: Load total fatigue life data

## Slide 30: Now fit the small fatigue crack
Constants to adjust for for small fatigue crack growth

## Slide 31: Decrease CII (HCF) until the “small crack” is in good agreement. (CII=0.0035)
Decrease CII to 0.0035
Set m=4.46
Based on experiments
LCF Range

## Slide 32: Increase CI (LCF) until the “small crack” curve is in good agreement. (CI=170000)
Increase CI to 170000
LCF Range

## Slide 33: 7075-T651 particle size range: 40-2mm. Enter large particle size to predict the lower bound (PT size= 40mm).
Curve shifts left

## Slide 34: 7075-T651 particle size range: 40-2mm. Enter Smaller particle size predict the upper bound (PT size= 2mm).
Curve shifts right

## Slide 35: Write a restart file

## Slide 36: MSFfit Overview
Notes: In this presentation:
The relationship between the plasticity-damage model (DMG), and the model calibration tool (DMGfit)
Implementations of DMGfit: for users on stand-alone PCs, or for Web-based users
The overall model calibration strategy
The calibration process specific to the DMG
The mapping of the calibration process to the DMGfit GUI
Labor saving features in the GUI, requested by MSU researchers
DMGfit demo